	2024 ASBESTOS REGISTER – HEALTH (Building 19), Rockhampton Girls Grammar School  
Date of register: 29/10/2024
NOTE: A demolition or refurbishment survey should be carried out by a competent person before undertaking refurbishment or demolition work.

	Workplace address:
	Rockhampton Girls 
Grammar School –
Denham Street, 
Rockhampton City QLD 4700
	Name and contact details of competent person:
	Lawrence Lyons
Asbestos Assessor Licence No. 2317266

Environics (QLD) Pty Ltd
ABN 76 354 368 913
Tel. 0429 128 145

	Workplace owner / manager:
	Kasey Mitchell
Facilities and Services Manager Rockhampton Girls Grammar School 
Tel. 0427 414 819

	Areas not assessed:
	Ceiling cavities located beyond inspection openings, utility pits, and elevated areas where safety measures cannot be practically implemented.

	Asbestos related 
documents:
	ENV-2023-062  Ver 1-4 Asbestos Management Plan & ACM Register - RGGS, Denham St The Range Q 4700.pdf   
· Appendix One	ENV-2023-062-RGGS-ASBESTOS REGISTER-v1-02.10.2024. (this document)
· Appendix Two         RGGS-691-PRO-ASBESTOS-MANAGEMENT-PROCEDURE-v1-24.07.2024
· Appendix Three      RGGS-692-PRO-ASBESTOS-INCIDENT-MANAGEMENT-PROCEDURE-v1-24.07.2024
· Appendix Four       RGGS-720-GDL-ASBESTOS-MANAGEMENT-POSTER-v1-24.07.2024


	Consultation:
	Attach minutes of relevant future meeting to this document.

	Disclaimer and 
Limitations:
	Inspections were limited to accessible areas without dismantling or removing objects, including vegetation, insulation, coverings, furnishings, and personal belongings. Areas such as inside walls, between floors, and behind stored items were not inspected. No destructive procedures were performed, and relevant legislation was followed. For further details on regulations, please refer to additional materials. Compliance and Liability: This register does not serve as a 'Certificate of Compliance' unless specified and does not warranty against future asbestos issues. The report does not confirm that all areas are asbestos-free. The competent person is not liable for undetectable asbestos requiring structural disruption. 

	

Date
	
Sample       No.
	Type of material identified or assumed and amount 
(Cross-sectional areas
 are estimates – measure before quoting)
	
Friable or non-friable asbestos
	

Condition of asbestos
	
Specific location of identified or assumed asbestos
	


Notes

	
06/10/2024
	
31
	
Chrysotile & Amosite 
	
Non-friable 

	
Good condition, painted
	
Interior: 
Ceilings of veranda – level one
	
COHLABS Certificate of Analysis No. 24-11633

	
06/10/2024
	
32
	
Chrysotile & Amosite 
	
Non-friable 

	
Good condition, painted
	
Interior: 
Ceilings of recovery room – level one
	
COHLABS Certificate of Analysis No. 24-11633

	Reinspection
19/10/2024
	GF-H1-2
	
Chrysotile & Amosite 
	

Non-friable 

	
Good condition, painted
	
Interior:
East wall to the workshop below the Health Centre 
	
SLR report 19/10/2023 
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Date
	
Sample       No.
	Type of material identified or assumed and amount 
(Cross-sectional areas
 are estimates – measure before quoting)
	
Friable or non-friable asbestos
	

Condition of asbestos
	
Specific location of identified or assumed asbestos
	


Notes

	Reinspection
19/10/2024
	
H2
	
Chrysotile 
	
Non-friable 
	
Not Found 
	
Interior:
NOT FOUND - Black backing board to the fuse board beneath the building

	
SLR report 19/10/2023 - Believed removed after 2013  


	Reinspection
19/10/2024
	
GF-H3-2.
	
Chrysotile & Amosite
	
Non-friable 
	Good condition, painted

	
Interior:
West wall sheeting 
	
SLR report 19/10/2023 – remains 


	Reinspection
19/10/2024
	
GF-H3-3.
	
Chrysotile & Amosite
	
Non-friable
	
Good condition, painted

	
Exterior:
 South wall sheeting of level one

	
SLR report 19/10/2023 – remains
All external wall sheeting considered to contain asbestos


	Reinspection
19/10/2024
	
H4
	
Chrysotile 
	
Non-friable
	
Not Found 
	Interior:

Vinyl flooring – level one 
	
SLR report 19/10/2023 - Believed removed after 2013  



	Reinspection
19/10/2024
	
H5
	
Chrysotile
	
Non-friable
	
Good condition, painted

	Interior:

Wall sheeting to Kitchen & Dining Area of Health Centre, Common to the Verandah & Staircase 
	
SLR report 19/10/2023 – remains 
Note: top of stairwell on left, no asbestos detected in this sheeting i.e. mixed sheeting may exist. 

	Reinspection
19/10/2024
	
RL-H8-1
	
Chrysotile
	
Non-friable
	
Good condition, painted

	
Exterior:
Eaves at the southern end, outside the dining room 
	
SLR report 19/10/2023 – remains 


	Reinspection
19/10/2024
	
RL-H8-2
	
Chrysotile
	
Non-friable
	
Good condition, painted

	
Exterior:
Eaves at the northern end of the building outside the classroom 
	
SLR report 19/10/2023 – remains 


	Reinspection
19/10/2024
	
RL-H8-3
	
Chrysotile
	
Non-friable
	
Good condition, painted

	Exterior:

Gables at the western end of the building 
	
SLR report 19/10/2023 – remains
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	NON-ASBESTOS MATERIALS

The following materials were tested and found not to contain asbestos:


	Date 
	Sample
No.
	Result of Analysis
	Location 
	Notes

	
Reinspection
19/10/2024
	
31
	No asbestos detected in sample. 
Organic fibres detected
	Interior:
Walls adjacent to stairwell leading to level one.  
	
COHLABS Certificate of Analysis No. 24-11633

	Reinspection
19/10/2024
	GF-H1-1
	No asbestos detected in sample.
Organic fibres detected
	Interior:
Sampling found the north and
south walls to be asbestos free
	SLR report 19/10/2023 


	Reinspection
19/10/2024
	GF-H1-3.
	No asbestos detected in sample.
Organic fibres detected
	Interior:
South wall to the workshop below the Health Centre 
	SLR report 19/10/2023 


	Reinspection
19/10/2024
	GF-H3-1.
	No asbestos detected in sample.
Organic fibres detected
	Exterior:
West wall sheeting – level one 
	SLR report 19/10/2023 
Sampling found the west inner and southern lower ground external walls to contain asbestos, while the external west outer wall does not contain asbestos.

	Reinspection
19/10/2024
	LP 1 & 2
	No asbestos detected in sample.
Organic fibres detected
	Exterior:
Cover strips to external wall sheeting of the building 
	SLR report 19/10/2023 
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